Polyjoiner Technical Notes

Unable to flash EBB42 successfully. Never boots to Marlin.

Punting the Creality V2.5.2 board from Creality CR-10 V2.
Building with Marlin-Makaira, but my build requires 170% of RAM using bugfix-2.1.x. Using 2.1.x only 52% so it’s a bugfix problem?
Board is RAMPS_CREALITY and display is REPRAP_DISCOUNT_FULL_GRAPHIC_SMART_CONTROLLER. And [XYZE]_DRIVER_TYPE is TMS2208_STANDALONE.
Can’t disable X_HOME_DIR in 2.1.x because it fails sanity check.

Alextrical’s Makefile has wrong board file number.
Boards.h has duplicate board numbers

## Polywelder version 0
Theory of Operation. Heat ends to be welded against a nozzle at Tm, extrude plastic in the gap to weld. Cool weld below Tg. Pull weld back and forth through another nozzle, 1.75 to 2 mm diameter, to re-form the weld.

- Tg of 223 C worked well to reform a single malformed end. Never got a good weld to test reforming a weld.
- Ends need heated to Tm in order to get a good weld. Extruding filament in the gap may be optional.
- Nearly impossible to align two ends by hand.
- Very hard to pull back and forth by hand if the rig is not fixed because it requires two hands to pull and one to hold the rig.
## Version 1
- Maybe silicone tube up to the Tg nozzle, with a small gap.
- Instead of nozzle, thin heated strip of copper that is inserted between the two ends, then pulled back. Maybe that strip has a 2mm hole when pulled back so there’s no gap between the silicone and the Tg nozzle.